## Slide 1
Fluorinated nanocarbons as promising additives for lubrication
1 Groupe de Technologie des Surfaces et Interfaces (GTSI), EA 2432, Université des Antilles, 97159 Pointe à Pitre Cedex, France
2 Centre Commun de Caractérisation des Antilles et de la Guyane, Université des Antilles, 97159 Pointe à Pitre Cedex, France
3 Institut de Chimie de Clermont-Ferrand, UMR CNRS-6002, Université Blaise Pascal de Clermont-Ferrand, 63177 Aubière , France
P. Thomas1, J.L. Mansot1,2, A. Molza2, K. Guérin3, M. Dubois3

## Slide 2
A few words about tribology
Energy losses
30% of produced energy in
the world is lost by friction
Relative movement of two contacting surfaces: friction and wear
Materials losses
66 million euros/year in France
Tribology: part of science concerned with friction, wear and
lubrication processes involved in many natural and industrial
domains
Lubrication: prevents contact between sliding surfaces
Notes: Billion = milliards

## Slide 3
Liquid lubricant: base + additives
Base: mineral or synthetic oil
Antiwear additive
Friction reducer
Corrosion inhibitor
Viscosity action
Additives
Anti-oxidizing action
Lubrication regimes

## Slide 4
Base: mineral or synthetic oil
Antiwear additive
Friction reducer
Corrosion inhibitor
Viscosity action
Additives
Anti-oxidizing action
Liquid lubricant: base + additives
Lubrication regimes
4 lubrication regimes
Sliding speed of moving surfaces
Lubricant viscosity
Normal load

## Slide 5
Friction coefficient (µ)
Elasto-HydroDynamic regime
HydroDynamic regime
Mixed regime
Film thickness (h)
ηV/FN
Boundary regime
h : Lubricant viscosity
FN : Normal load
V : Sliding speed
Friction reduction due to
Additives
Base +
Additives
Base
Base
Fn
Ft
Lubrication regimes

## Slide 6
Friction coefficient (µ)
Elasto-HydroDynamic regime
HydroDynamic regime
Mixed regime
Film thickness (h)
ηV/FN
Boundary regime
h : Lubricant viscosity
FN : Normal load
V : Sliding speed
Friction reduction due to
Additives
Base +
Additives
Base
Base
Fn
Ft
Lubrication regimes
Ball bearings
High friction coefficient
Severe wear

## Slide 7
Friction coefficient (µ)
Elasto-HydroDynamic regime
HydroDynamic regime
Mixed regime
Film thickness (h)
ηV/FN
Boundary regime
h : Lubricant viscosity
FN : Normal load
V : Sliding speed
Friction reduction due to
Additives
Base +
Additives
Base
Base
Fn
Ft
Lubrication regimes
Engines
Performances due to antiwear and friction reduction additives
High friction coefficient
Severe wear

## Slide 8
Conventional friction reduction
and antiwear additives
Conventional additives: Zinc DialkylDithiophosphate (ZDDP),
Molybdenum Dithiophosphate (MoDTP) or Dithiocarbamate (MoDTC)
Built up of a protective tribofilm resulting from chemical
reactions between additives molecules and surfaces
Tribofilm
Additives molecules
- The tribofilm is not immediately built (induction period)  severe wear undergone
by the substrates
The protective action is not efficient in the case of non-reactive sliding surfaces
(ceramics,…)
But

## Slide 9
New lubrication strategies
New additives: micro/nanoparticles of tribo-active phases (graphite,
MoS2) or precursors of tribo-active phases (C and inorganic
nanotubes or fullerenes) dispersed in the lubricant base
Phases are selected according to their intrinsic friction
properties
Graphite: m = 0,1 CFx: m = 0,09
Good lubricant
if m ≤ 0,1
Good thermal stability
High chemical stability
Anticorrosive and
hydrophobic properties
Good friction properties
Fluorinated carbons
van der Waals
gap

## Slide 10
New lubrication strategies
New additives: micro/nanoparticles of tribo-active phases (graphite,
MoS2) or precursors of tribo-active phases (C and inorganic
nanotubes or fullerenes) dispersed in the lubricant base
Immediate formation of the tribofilm in the sliding contact
conditions without any chemical reactions with the substrates
The induction period strongly depends on the size
of the particles: feeding of the sliding interface
Synthetic graphite
Study of fluorinated nanocarbons
Carbon Nanodiscs
(CNDs)
2D structure
Tubular 1D structure
Spherical 0D structure
Carbon Nanofibers
(CNFs)
Graphitized Carbon Blacks
(GCBs)

## Slide 11
Tribologic experimental device
Motor
Sphere
Plane
x,y,z sample
holder
AISI 52100
steel ball
Normal load Fn
Measurement of
the lateral force Ft
Ft
AISI 52100
steel plane
Fluorinated carbon film
Normal load: 10 N
Contact area diameter: 140 mm
Maximum contact Pressure: 1 GPa
- Sliding speed: 6 mm/s
Friction coefficient m = Ft / Fn
Friction coefficient
Cycles number
Friction coefficient
Cycles number
m = (a-b)/2
The ball goes forward
The ball moves back
The ball stops ans reverses
Plane
Cycle = reciprocal travel of the ball on the static plane

## Slide 12
Nanocarbons fluorination
Fluorination under F2 atmosphere at selected temperatures in order
to obtain controlled fluorine contents (expressed as atomic F/C ratio)
Starting material | TF range (°C) | F/C range*
CNDs | 450-520 | 0.14-1.0
CNFs | 380-480 | 0.06–1.04
GCBs | 320-340 | 0.08-1.04
Carbon Nanodiscs (CNDs)
Carbon Nanofibers (CNFs)
Graphitized Carbon Blacks (GCBs)
F/C ≈ 1
F/C ≈ 1
F/C ≈ 1
*F/C ratios were determined by weight uptake or 13C and 19F NMR
Covalent C-F bonds

## Slide 13
Tribologic properties of fluorinated nanocarbons
 Fluorination improves the friction
properties
mfluorinated materials < mpristine compounds
Linear decrease of m for
0 < F/C < 0.15 for CNFs and
0 < F/C < 0.6 for CBGs
Stabilization at m  0.08 for
higher F/C ratios
 Carbon nanofibers (CNFs) and
graphitized carbon blacks (GCBs):
the friction properties depend on
the fluorine content
m  0.08 for all the tested
compounds
 Carbon nanodiscs (CNDs): the
friction properties do not depend on
the fluorine content

## Slide 14
Tribologic properties of fluorinated nanocarbons
Fluorinated nanocarbons
present excellent friction
reduction properties
Different friction reduction
mechanisms
 Very low values of m
Different tribologic behaviour
depending on the morphology of
the particles

## Slide 15
Friction reduction mechanisms
Friction reduction mechanisms of CNFs: correlation between friction
properties and structural characterizations
 Lattice fringes corresponding
to graphitic structure are
visible in the internal part of
the fiber
 Presence of fluorine at the
periphery
Progressive fluorination proceeding from the outer part of the carbon nanofiber towards its core as far as the fluorination temperature increases
TEM investigation of a cross section of a fluorinated CNF
F/C = 0.15

## Slide 16
Friction reduction mechanisms
Friction reduction mechanisms of CNFs: correlation between friction
properties and structural characterizations
Fluorination  Decrease of surface
free energy: minimum obtained for
F/C  0.15
Fluorination progresses towards the
fibres core : no significant evolution
of the surface free energy
 m for F/C < 0.15
 m  0.08 for F/C > 0.15
CNFs
Friction reduction mechanism involving
surface effects (individual nanofibers
interactions)

## Slide 17
Friction reduction mechanisms
Friction reduction mechanisms of GCBs: correlation between friction
properties and structural characterizations
TEM characterization of fluorinated GCBs
 Pristine materials present a graphitic structure
 The fluorinated parts are characterized by an increase of the interplanar distance (d = 0.48 nm) compared to graphite one (d = 0.34 nm)
Pristine CBGs
CF0.16
CF0.89
d = 0.34 nm
Fluorinated layers
d = 0.48 nm
Graphene layers
d = 0.34 nm

## Slide 18
Friction reduction mechanisms
Friction reduction mechanisms of GCBs: correlation between friction
properties and structural characterizations
TEM characterization of fluorinated GCBs
Pristine CBGs
CF0.16
CF0.89
d = 0.34 nm
Fluorinated layers
d = 0.48 nm
Graphene layers
d = 0.34 nm
The fluorination process progresses from external layers towards inner ones

## Slide 19
Friction reduction mechanisms
Friction reduction mechanisms of GCBs: correlation between friction
properties and structural characterizations
 Decrease of m associated to the
lowering of surface energy of the
particles due to the thickening of
the fluorinated layer
 The thickness of the surrounding
fluorinated layer is sufficient to
stabilize the surface energy of the
particles
No more surface effects: stabilization
of the friction coefficient
Friction reduction mechanism involving surface effects

## Slide 20
Friction reduction mechanisms
Friction reduction mechanisms of CNDs: correlation between friction
properties and structural characterizations
TEM Characterization
AFM investigations
F/C = 0.78
 Swelling is more pronounced at the edges of the nanodiscs
 Swelling of the edges is visible in the overall perimeter
The fluorination process mainly occurs via the edges of the CNDs

## Slide 21
Friction reduction mechanisms
Friction reduction mechanisms of CNDs: correlation between friction
properties and structural characterizations
 Fluorination occurs via the edges: the fluorine atoms diffuse in the whole volume
The friction coefficient does not depend on the fluorine content: friction
reduction mecanisms implying bulk effects
F2
F2
CND
F/C = 0.78

## Slide 22
Antiwear properties of fluorinated nanocarbons
GCBs
CF0.16 1000 cycles
Initial scratches
GCBs
CF0.89 1000 cycles
Initial scratches
 Initial scratches are still visible after 1000 cycles of friction: very weak wear
 Same observations for all the tested compounds
Fluorinated nanocarbons present good antiwear properties

## Slide 23
Conclusions
 Promising new nano-additives for liquid or gel lubricants
- Very low friction coefficient: m ≈ 0.08
- Very good durability of the friction performances
- Instantaneous protective action: no induction period
 Fluorination improves the friction performances of nanocarbons
 Friction reduction mechanisms depend on the morphology of the particles
Surface effects
Carbon nanofibers (1D)
graphitized carbon blacks (0D)
Bulk effects
Carbon nanodiscs (2D)
- Sizes and geometries well adapted for a good feeding of the sliding interface
- Good antiwear properties

## Slide 24
Thank you for your attention
ACKNOWLEDGEMENTS: The authors acknowledge the CNRS, the Conseil Régional de la Guadeloupe, the Fond Social Européen (FSE) and Fonds Européens de Développement Régional (FEDER) for their financial supports.

## Slide 26
Friction reduction mechanisms
Study of the tribofilms: SEM investigations
High contact pressure zone:
very smooth aspect
Low contact pressure zone: the discs
are oriented parallel to the sliding
direction
1 mm
Carbon nanodiscs
Aspect of the tribofilm
Particles extracted from
the wear scar
2 mm
Individual nanodiscs
The tribofilm is mainly amorphous
with some individual discs
embedded in the disordered phase
Ball
Plane
Tribofilm
High pressure zone
Low pressure
zone

## Slide 27
Friction reduction mechanisms
Low contact pressure zone: orientation
of the fibers along the sliding direction
High pressure zone: continuous
aspect with ondulations
Tangled fibers
Pristine CNFs
b)
Pristine CNFs
Pristine CNFs
F/C = 0.39
Tribofilms constituted of individual
nanofibers covered by an ill organized
layer (0.3 mm thickness)
Study of the tribofilms: SEM investigations
Carbon nanofibers
Aspect of the tribofilm
Particles extracted from
the wear scar
Ball
Plane
Tribofilm
High pressure zone
Low pressure
zone

## Slide 28
Friction reduction mechanisms
high
pressure zone
0.2 mm
Tribofilms seems to be
constituted of individual
CBGs embedded in a
disordered phase
Study of the tribofilms: SEM investigations
Graphitized carbon blacks
Aspect of the tribofilm
Wear scar
2 mm
Low
pressure zone
Ball
Plane
Tribofilm
High pressure zone
Low pressure
zone